SECTION 079200 - JOINT SEALANTS (Very Low VOC as Indicated: Section 2.3.E)

PART 1 - GENERAL

  - RELATED DOCUMENTS

    - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

  - SUMMARY

    - This Section includes joint sealants for the applications indicated in the Joint-Sealant Schedule at the end of Part 3.

      - Exterior joints in the following vertical surfaces and horizontal nontraffic surfaces:

        - Control and expansion joints in unit masonry.

        - Joints in dimension stone cladding.

        - Joints in glass unit masonry assemblies.

        - Joints in exterior portland cement stucco

        - Joints between metal panels.

        - Joints between different materials listed above.

        - Perimeter joints between materials listed above and frames of doors, windows and louvers.

        - Control joints in ceilings and other overhead surfaces.

        - Other joints as indicated.

      - Exterior joints in the following horizontal traffic surfaces:

        - Isolation and contraction joints in cast-in-place concrete slabs.

        - Joints between different materials listed above.

        - Other joints as indicated.

      - Interior joints in the following vertical surfaces and horizontal nontraffic surfaces:

        - Control joints on exposed interior surfaces of exterior walls.

        - Perimeter joints of exterior openings where indicated.

        - Vertical joints on exposed surfaces of interior unit masonry walls and partitions.

        - Perimeter joints between interior wall surfaces and frames of interior doors, windows and elevator entrances.

        - Joints between plumbing fixtures and adjoining walls, floors, and counters.

        - Other joints as indicated.

      - Interior joints in the following horizontal traffic surfaces:

        - Isolation joints in cast-in-place concrete slabs.

        - Control joints in tile flooring.

        - Other joints as indicated.

    - Related Sections include the following:

      - Division 04 Section "Unit Masonry" for masonry control and expansion joint fillers and gaskets.

      - Division 07 Section "Fire-Resistive Joint Systems" for sealing joints in fire-resistance- rated construction.

      - Division 08 Section "Glazing" for glazing sealants.

      - Division 09 Section "Portland Cement Stucco" for sealing perimeter joints of gypsum veneer plaster partitions to reduce sound transmission.

      - Division 09 Section "Gypsum Board" for sealing perimeter joints of gypsum board partitions to reduce sound transmission.

      - Division 09 Section "Tiling" for sealing tile joints.

      - Division 09 Section "Acoustical Panel Ceilings" for sealing edge moldings at perimeters of acoustical ceilings.

  - PERFORMANCE REQUIREMENTS

    - Provide elastomeric joint sealants that establish and maintain watertight and airtight continuous joint seals without staining or deteriorating joint substrates.

    - Provide joint sealants for interior applications that establish and maintain airtight and water- resistant continuous joint seals without staining or deteriorating joint substrates.

  - SUBMITTALS

    - Product Data: For each joint-sealant product indicated.

    - Samples for Initial Selection: Manufacturer's color charts consisting of strips of cured sealants showing the full range of colors available for each product exposed to view.

    - Samples for Verification: For each type and color of joint sealant required, provide Samples with joint sealants in 1/2-inch- (13-mm-) wide joints formed between two 6-inch- (150-mm-) long strips of material matching the appearance of exposed surfaces adjacent to joint sealants.

    - Product  Certificates:	For each type of joint sealant and accessory, signed by product manufacturer.

    - Qualification Data: For Installer.

    - Compatibility and Adhesion Test Reports: From sealant manufacturer, indicating the following:

      - Materials forming joint substrates and joint-sealant backings have been tested for compatibility and adhesion with joint sealants.

      - Interpretation of test results and written recommendations for primers and substrate preparation needed for adhesion.

  - QUALITY ASSURANCE

    - Source Limitations: Obtain each type of joint sealant through one source from a single manufacturer.

    - Perform work in accordance with sealant manufacturer’s requirements for preparation of surfaces and material installation instructions.

    - Perform acoustical sealant application work in accordance with ASTM C919.

    - Product Testing: Obtain test results for "Product Test Reports" Paragraph in "Submittals" Article from a qualified testing agency based on testing current sealant formulations within a 36-month period preceding the commencement of the Work.

      - Test elastomeric joint sealants for compliance with requirements specified by reference to ASTM C 920, and where applicable, to other standard test methods.

      - Test elastomeric joint sealants according to SWRI's Sealant Validation Program for compliance with requirements specified by reference to ASTM C 920 for adhesion and cohesion under cyclic movement, adhesion-in-peel, and indentation hardness.

    - Mockups: Build mockups incorporating sealant joints, as follows, to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution:

      - Joints in mockups of assemblies specified in other Sections that are indicated to receive elastomeric joint sealants, which are specified by reference to this Section.

  - PROJECT CONDITIONS

    - Do not proceed with installation of joint sealants under the following conditions:

      - When ambient and substrate temperature conditions are outside limits permitted by joint- sealant manufacturer or are below 40 deg F (5 deg C).

      - When joint substrates are wet.

      - Where joint widths are less than those allowed by joint-sealant manufacturer for applications indicated.

      - Contaminants capable of interfering with adhesion have not yet been removed from joint substrates.

  - WARRANTY

    - Special Installer's Warranty: Installer's standard form in which Installer agrees to repair or replace elastomeric joint sealants that do not comply with performance and other requirements specified in this Section within specified warranty period.

      - Warranty Period: Two years from date of Substantial Completion.

    - Special Manufacturer's Warranty: Manufacturer's standard form in which elastomeric sealant manufacturer agrees to furnish elastomeric joint sealants to repair or replace those that do not

comply with performance and other requirements specified in this Section within specified warranty period.

      - Warranty Period: Two years from date of Substantial Completion.

    - Special warranties specified in this Article exclude deterioration or failure of elastomeric joint sealants from the following:

      - Movement of the structure resulting in stresses on the sealant exceeding sealant manufacturer's written specifications for sealant elongation and compression caused by structural settlement or errors attributable to design or construction.

      - Disintegration of joint substrates from natural causes exceeding design specifications.

      - Mechanical damage caused by individuals, tools, or other outside agents.

      - Changes in sealant appearance caused by accumulation of dirt or other atmospheric contaminants.

PART 2 - PRODUCTS

  - MANUFACTURERS

    - Products: Subject to compliance with requirements, provide one of the products listed in other Part 2 articles.

  - MATERIALS, GENERAL

    - Compatibility: Provide joint sealants, backings, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by sealant manufacturer, based on testing and field experience.

    - VOC Content of Interior Sealants: Provide interior sealants and sealant primers that comply with the following limits for VOC content when calculated according to 40 CFR 59, Subpart D (EPA Method 24):

      - Sealants: 250 g/L.

      - Sealant Primers for Nonporous Substrates: 250 g/L.

      - Sealant Primers for Porous Substrates: 775 g/L.

    - Colors of Exposed Joint Sealants: As selected by Architect from manufacturer's full range.

  - ELASTOMERIC JOINT SEALANTS

    - Elastomeric Sealants: Comply with ASTM C 920 and other requirements indicated for each liquid-applied chemically curing sealant specified, including those referencing ASTM C 920 classifications for type, grade, class, and uses related to exposure and joint substrates.

    - Stain-Test-Response Characteristics: Where elastomeric sealants are specified to be  nonstaining to porous substrates, provide products that have undergone testing according to ASTM C 1248 and have not stained porous joint substrates indicated for Project.

    - Suitability for Immersion in Liquids. Where elastomeric sealants are indicated for Use I for joints that will be continuously immersed in liquids, provide products that have undergone testing according to ASTM C 1247 and qualify for the length of exposure indicated by reference to ASTM C 920 for Class 1 or 2. Liquid used for testing sealants is deionized water, unless otherwise indicated.

    - Suitability for Contact with Food: Where elastomeric sealants are indicated for joints that will come in repeated contact with food, provide products that comply with 21 CFR 177.2600

    - Single-Component Non-sag Polyether Sealant ES-A (Very Low VOC [less than 2%]):

1.	Available Products Very Low VOC (less than 2%)

STS Coatings, GreatSeal PE-.150 (830-995-5177) Sonneborn, Division of BASF: Sonolastic 150.

a.

b.

Uses  Related  to  Joint  Substrates:	M, G, A, and, as applicable to joint substrates

5.

Use Related to Exposure: NT (nontraffic).

4.

Class: 25.

3.

Type and Grade: S (single component) and NS (nonsag).

2.

indicated, O.

a.	Use O Joint Substrates: galvanized steel, brick, and concrete.

- Stain-Test-Response	Characteristics:	Nonstaining	to	porous	substrates	per ASTM C 1248.

- Exterior Gypsum Joint Sealants (Very Low VOC less than 2%) (IECC Required)

  - LT-100 Sealant by STS Coatings (830-995-5177) b.	UniverSeal by York Mfg. (800-551-2828)

    - Single-Component Neutral-Curing Silicone Sealant ES- B:

      - Available Products:

        - Sonneborn, Division of ChemRex Inc., BASF; Omniseal 50.

        - Dow Corning Corporation; 795

        - GE Silicones; SilPruf NB SCS9000.

        - Pecora Corporation; 895.

      - Type and Grade: S (single component) and NS (nonsag).

      - Class: 50.

      - Use Related to Exposure: NT (nontraffic).

      - Uses  Related  to  Joint  Substrates:	M, G, A, and, as applicable to joint substrates indicated, O.

        - Use O Joint Substrates: Glass and color anodic aluminum.

    - Single-Component Acid-Curing Silicone Sealant ES-C:

      - Available Products:

        - Dow Corning Corporation; 999-A.

        - GE Silicones; Sanitary SCS1700.

        - Pecora Corporation; 860..

        - Sonneborn, Division of ChemRex Inc.; OmniPlus.

        - Tremco; Tremsil 200.

      - Type and Grade: S (single component) and NS (nonsag).

      - Class: 25.

      - Use Related to Exposure: NT (nontraffic).

      - Uses Related to Joint Substrates: G, A, and, as applicable to joint substrates indicated, O.

        - Use O Joint Substrates: ceramic tile and stainless steel.

    - Multicomponent Nonsag Urethane Sealant ES-D:

      - Available Products:

        - Sonneborn, Division of ChemRex Inc.; NP 2.

      - Type and Grade: M (multicomponent) and NS (nonsag).

      - Class: 25.

      - Uses Related to Exposure: T (traffic) and NT (nontraffic).

      - Uses  Related  to  Joint  Substrates:	M, G, A, and, as applicable to joint substrates indicated, O.

        - Use O Joint  Substrates:	Color anodic aluminum, galvanized steel, brick, and ceramic tile.

    - Multicomponent Pourable Urethane Sealant ES-E:

      - Available Products:

        - Pecora Corporation; Dynatrol II-SG.

        - Sika Corporation, Inc.; Sikaflex - 2c SL.

        - Sonneborn, Division of ChemRex Inc.; SL 2.

      - Type and Grade: M (multicomponent) and P (pourable).

      - Class: 25.

      - Uses Related to Exposure: T (traffic) and NT (nontraffic).

      - Uses  Related  to  Joint  Substrates:	M, G, A, and, as applicable to joint substrates indicated, O.

        - Use O Joint Substrates: ceramic tile and concrete.

  - ACOUSTICAL JOINT SEALANTS

    - Acoustical Sealant for Exposed and Concealed Joints AS-A: Manufacturer's standard nonsag, paintable, nonstaining latex sealant complying with ASTM C 834 and the following:

      - Product effectively reduces airborne sound transmission through perimeter joints and openings in building construction as demonstrated by testing representative assemblies according to ASTM E 90.

      - Available Products:

        - Pecora Corporation; AC-20 FTR Acoustical and Insulation Sealant.

        - United States Gypsum Co.; SHEETROCK Acoustical Sealant.

  - JOINT-SEALANT BACKING

    - General: Provide sealant backings of material and type that are nonstaining; are compatible  with joint substrates, sealants, primers, and other joint fillers; and are approved for applications indicated by sealant manufacturer based on field experience and laboratory testing.

    - Cylindrical Sealant Backings: ASTM C 1330, Type C (closed-cell material with a surface  skin), and of size and density to control sealant depth and otherwise contribute to producing optimum sealant performance:

    - Elastomeric Tubing Sealant Backings: Neoprene, butyl, or silicone tubing complying with ASTM D 1056, nonabsorbent to water and gas, and capable of remaining resilient at temperatures down to minus 26 deg F (minus 32 deg C). Provide products with low compression set and of size and shape to provide a secondary seal, to control sealant depth, and to otherwise contribute to optimum sealant performance.

    - Bond-Breaker Tape: Polyethylene tape or other plastic tape recommended by sealant manufacturer for preventing sealant from adhering to rigid, inflexible joint-filler materials or joint surfaces at back of joint where such adhesion would result in sealant failure. Provide self- adhesive tape where applicable.

  - MISCELLANEOUS MATERIALS

    - Primer: Material recommended by joint-sealant manufacturer where required for adhesion of sealant to joint substrates indicated, as determined from preconstruction joint-sealant-substrate tests and field tests.

    - Cleaners for Nonporous Surfaces: Chemical cleaners acceptable to manufacturers of sealants and sealant backing materials, free of oily residues or other substances capable of staining or harming joint substrates and adjacent nonporous surfaces in any way, and formulated to promote optimum adhesion of sealants to joint substrates.

    - Masking Tape: Nonstaining, nonabsorbent material compatible with joint sealants and surfaces adjacent to joints.

PART 3 - EXECUTION

  - EXAMINATION

    - Examine joints indicated to receive joint sealants, with Installer present, for compliance with requirements for joint configuration, installation tolerances, and other conditions affecting joint- sealant performance.

    - Proceed with installation only after unsatisfactory conditions have been corrected.

  - PREPARATION

    - Surface Cleaning of Joints: Clean out joints immediately before installing joint sealants to comply with joint-sealant manufacturer's written instructions and the following requirements:

      - Remove all foreign material from joint substrates that could interfere with adhesion of joint sealant, including dust, paints (except for permanent, protective coatings tested and approved for sealant adhesion and compatibility by sealant manufacturer), old joint sealants, oil, grease, waterproofing, water repellents, water, surface dirt, and frost.

      - Clean porous joint substrate surfaces by brushing, grinding, blast cleaning, mechanical abrading, or a combination of these methods to produce a clean, sound substrate capable of developing optimum bond with joint sealants. Remove loose particles remaining after cleaning operations above by vacuuming or blowing out joints with oil-free compressed air. Porous joint substrates include the following:

        - Concrete.

        - Masonry.

        - Unglazed surfaces of ceramic tile.

      - Remove laitance and form-release agents from concrete.

      - Clean nonporous surfaces with chemical cleaners or other means that do not stain, harm substrates, or leave residues capable of interfering with adhesion of joint sealants. Nonporous joint substrates include the following:

        - Metal.

        - Glass.

        - Porcelain enamel.

        - Glazed surfaces of ceramic tile.

    - Joint Priming: Prime joint substrates, where recommended in writing by joint-sealant manufacturer, based on preconstruction joint-sealant-substrate tests or prior experience. Apply primer to comply with joint-sealant manufacturer's written instructions. Confine primers to areas of joint-sealant bond; do not allow spillage or migration onto adjoining surfaces.

    - Masking Tape: Use masking tape where required to prevent contact of sealant with adjoining surfaces that otherwise would be permanently stained or damaged by such contact or by cleaning methods required to remove sealant smears. Remove tape immediately after tooling without disturbing joint seal.

  - INSTALLATION OF JOINT SEALANTS

    - General: Comply with joint-sealant manufacturer's written installation instructions for products and applications indicated, unless more stringent requirements apply.

    - Sealant Installation Standard: Comply with recommendations in ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions indicated.

    - Acoustical Sealant Application Standard: Comply with recommendations in ASTM C 919 for use of joint sealants in acoustical applications as applicable to materials, applications, and conditions indicated.

    - Install sealant backings of type indicated to support sealants during application and at position required to produce cross-sectional shapes and depths of installed sealants relative to joint widths that allow optimum sealant movement capability.

      - Do not leave gaps between ends of sealant backings.

      - Do not stretch, twist, puncture, or tear sealant backings.

      - Remove absorbent sealant backings that have become wet before sealant application and replace them with dry materials.

    - Install bond-breaker tape behind sealants where sealant backings are not used between sealants and backs of joints.

    - Install sealants using proven techniques that comply with the following and at the same time backings are installed:

      - Place sealants so they directly contact and fully wet joint substrates.

      - Completely fill recesses in each joint configuration.

      - Produce uniform, cross-sectional shapes and depths relative to joint widths that allow optimum sealant movement capability.

    - Tooling of Nonsag Sealants: Immediately after sealant application and before skinning or  curing begins, tool sealants according to requirements specified below to form smooth, uniform beads of configuration indicated; to eliminate air pockets; and to ensure contact and adhesion of sealant with sides of joint.

      - Remove excess sealant from surfaces adjacent to joints.

      - Use tooling agents that are approved in writing by sealant manufacturer and that do not discolor sealants or adjacent surfaces.

      - Provide concave joint configuration per Figure 5A in ASTM C 1193, unless otherwise indicated.

      - Provide flush joint configuration where indicated per Figure 5B in ASTM C 1193.

      - Provide recessed joint configuration of recess depth and at locations indicated  per  Figure 5C in ASTM C 1193.

        - Use masking tape to protect surfaces adjacent to recessed tooled joints.

    - Installation of Preformed Tapes: Install according to manufacturer's written instructions.

    - Installation of Preformed Silicone-Sealant System: Comply with the following requirements:

      - Apply masking tape to each side of joint, outside of area to be covered by sealant system.

      - Apply silicone sealant to each side of joint to produce a bead of size complying with preformed silicone-sealant system manufacturer's written instructions and covering a bonding area of not less than 3/8 inch (10 mm). Hold edge of sealant bead 1/4 inch (6 mm) inside masking tape.

      - Within 10 minutes of sealant application, press silicone extrusion into sealant to wet extrusion and substrate. Use a roller to apply consistent pressure and ensure uniform contact between sealant and both extrusion and substrate.

      - Complete installation of sealant system in horizontal joints before installing in vertical joints. Lap vertical joints over horizontal joints. At ends of joints, cut silicone extrusion with a razor knife.

    - Installation of Preformed Foam Sealants: Install each length of sealant immediately after removing protective wrapping, taking care not to pull or stretch material, producing seal continuity at ends, turns, and intersections of joints. For applications at low ambient temperatures where expansion of sealant requires acceleration to produce seal, apply heat to sealant in compliance with sealant manufacturer's written instructions.

  - FIELD QUALITY CONTROL

    - Field-Adhesion Testing: Field test joint-sealant adhesion to joint substrates as follows:

      - Extent of Testing: Test completed elastomeric sealant joints as follows:

        - Perform 10 tests for the first 1000 feet (300 m) of joint length for each type of elastomeric sealant and joint substrate.

        - Perform 1 test for each 1000 feet (300 m) of joint length thereafter or 1 test per each floor per elevation.

      - Test Method: Test joint sealants according to Method A, Field-Applied Sealant Joint Hand Pull Tab or Method D, Water Immersion in Appendix X1 in ASTM C 1193, as appropriate for type of joint-sealant application indicated.

        - For joints with dissimilar substrates, verify adhesion to each substrate separately; do this by extending cut along one side, verifying adhesion to opposite side. Repeat procedure for opposite side.

      - Inspect joints for complete fill, for absence of voids, and for joint configuration complying with specified requirements. Record results in a field-adhesion-test log.

      - Inspect tested joints and report on the following:

        - Whether sealants in joints connected to pulled-out portion failed to adhere to joint substrates or tore cohesively. Include data on pull distance used to test each type  of product and joint substrate. Compare these results to determine if adhesion passes sealant manufacturer's field-adhesion hand-pull test criteria.

        - Whether sealants filled joint cavities and are free of voids.

        - Whether sealant dimensions and configurations comply with specified requirements.

      - Record test results in a field-adhesion-test log. Include dates when sealants were installed, names of persons who installed sealants, test dates, test locations, whether joints were primed, adhesion results and percent elongations, sealant fill, sealant configuration, and sealant dimensions.

      - Repair sealants pulled from test area by applying new sealants following same procedures used originally to seal joints. Ensure that original sealant surfaces are clean and that new sealant contacts original sealant.

    - Evaluation of Field Test Results: Sealants not evidencing adhesive failure from testing or noncompliance with other indicated requirements will be considered satisfactory. Remove sealants that fail to adhere to joint substrates during testing or to comply with other requirements. Retest failed applications until test results prove sealants comply with indicated requirements.

  - CLEANING

    - Clean off excess sealant or sealant smears adjacent to joints as the Work progresses by methods and with cleaning materials approved in writing by manufacturers of joint sealants and of products in which joints occur.

  - PROTECTION

    - Protect joint sealants during and after curing period from contact with contaminating substances and from damage resulting from construction operations or other causes so sealants are without deterioration or damage at time of Substantial Completion. If, despite such protection, damage or deterioration occurs, cut out and remove damaged or deteriorated joint sealants immediately so installations with repaired areas are indistinguishable from original work.

| 3.7 JOINT-SEALANT SCHEDULE. |  |  |
| --- | --- | --- |
| Location | Type | Color |
| A. Window Perimeter, Frames, Storefront Or Curtain Wall Assembly | B | To Match Adjacent |
| B. Door Frames / Wall Perimeters | A | To Match Adjacent |
| C. Under Thresholds Under Window system which rests directly on the floor slab in order to prevent infiltration | A | Black |
| D. Toilet Room Fixtures, Accessories Ceramic Tile | C | White |
| E. Intersection of dissimilar materials that allows water or air infiltration | A | To Match Adjacent |
| F. Perimeter Joints on interior side of door Frames, louvers in exterior walls | A | To Match Adjacent |

| G. | Perimeter Joints of door frames, window frames And other framed openings in walls with no Finished edge flange. | A | To Match Adjacent |
| --- | --- | --- | --- |
| H. | Open Joints at penetrations through walls, and open joints at penetrations through concrete or gypsum board ceilings, where intended to be tight sealed joints | A | To Match Adjacent |
| I. | Open Joint, between dissimilar materials where intended to be tight, sealed joint. | A | To Match Adjacent |
| J. | Joints where edge trim of gypsum board abuts irregular surfaces or other surfaces and leaves open joint | A | To Match Adjacent |
| K. | Within and perimeter of Masonry System | A | To Match Adjacent |
| L. | Intersection of dissimilar materials which installations not uniform or where workmanship does not meet acceptable construction tolerances, when such workmanship is acceptable by the Architect. | A | To Match Adjacent |
| M. | Metal Siding, louvers, fixtures and other penetrations in building enclosures not otherwise sealed weathertight. Unless noted otherwise provide continuous sealing perimeter joints and all other joints at exterior soffits. | A | To Match Adjacent |
| N. | Paving Floors joints Expansion joints in and around concrete pavement, curbs, or other horizontal surfaces. In horizontal joints in concrete floor where intended to be tight, sealed joints. Expansion joints in concrete slabs, around column piers penetrating concrete slab, at all natural concrete slab expansion control points as specified | E | To Match Adjacent |
| O. | Within Glazing Systems | B | To Match Adjacent |
| P. | Within Roofing System | A, D | To Match Adjacent |

END OF SECTION 079200